## Slide 1: Electron spin relaxation effects of a single phosphorus donor in silicon at low temperatures: tunnel effects summary
Stefanie Tenberg,
Andrea Morello
CQC2T, UNSW
07/06/2018

## Slide 2: Tunnelling processes between donor and SET
|
|
|
|
First order tunnelling (direct tunnelling): exponentially suppressed with the donor distance to the Fermi level
Second order tunnelling (co-tunnelling):
Otsuka et. al. Scientific Reports 2017,
DOI:10.1038/s41598-017-12217-6

## Slide 3: Sequence to measure relaxation times
Pulse sequence
Initialization
Plunge
Read-out
Inversion
Plunge voltages,
Fixed SET level (compensated) in green
Non compensated in blue
0

## Slide 4: Relaxation rate with plunge depth
Plunge voltage here is distance ’ to the Fermi level

## Slide 5: Relate voltages to energy
mV @5T
lever arm
Zeeman splitting @1T: 14mV
Spin tail measurement gives the lever arm and the Zeeman splitting in volts

## Slide 6: Zoomed in
Fitting:
Direct is
Results:
Hz
Agrees with trace data
Co-tunnelling does not fit
What is going on here?
The exponential is a random fit we made up…

## Slide 10: Dependence of on SET electron number
T
Tunnelling effects depend on the Fermi distribution in the SET
The SET is with 𝑛≈100 in the intermediate regime between few and many electrons ⇒ the Fermi distribution has some variation with electron number

## Slide 11: Dependence of on SET electron number
For large plunge voltages all tunnelling processes are suppressed ⇒ relaxation is independent of electron number
These measurements show less of an exponential like for direct tunnelling expected
Uneven Fermi distribution?

## Slide 12: Questions for Bill
Do you have any idea what is going on for plunge voltages deeper than half the Zeeman energy?
It seems that we observe direct tunnelling until the spin up moves below the Fermi level – as expected. Below that there is still a drop of up at a factor of 5 until the relaxation rate reaches the phonon relaxation plateau. What is going on here?
Additional information:
Unfortunately this specific sample died so we cannot take any more measurements. Also, as we were changing over our measurement software at that time, we do not have the traces for this specific measurement set. Although we should have general traces somewhere to dig up, which I’m in the process of doing.